https://www.diyelectronics.co.za/store/exotics/197-cctree-flexible-tpu-filament-175mm-red.html

 CCTREE Flexible TPU Filament - 1.75mm Red
1 Review(s)
Reference HWPPFLEX1.75R
Condition: New

1kg Spools of 1.75mm Red Flexible TPU Filament from CCTREE – For printing bendable, flexible and stretchable parts, models and toys.

Within the world of 3D Printing, there are so many different types of 3D Printer Filaments to choose from, with new polymers coming out almost monthly. One such example of this is Red Flexible 1.75mm TPU Filament, which offers the unique characteristic of being flexible and durable against impacts and compression forces. With a shore hardness of between 90 and 98, this filament can be printed with an almost tyre-like feel, which can be “squished” quite dramatically while still reverting back to its original shape and form.
This flexible TPU filament is a polymer that utilises PLA as a base plastic, meaning it has very similar printing specifications to Standard PLA Filament. However, the added materials that give it the unique flexible traits means that the polymer does require some experimentation and practice to get just right. So, as a start, begin by raising the temperature of your hotend and heatbed by around 10 to 20 degrees, and set the machine to print at a slightly slower speed. From there, you will simply need to tweak the printing specifications until you are satisfied with the print quality, aiming for as little stringing and lifting as possible.

CCTREE Red Flexible 1.75mm TPU Filament - Technical Specifications:
Base Plastic Type	– TPU (Thermoplastic Polyurethane)
Plastic Colour	– Red
Filament Diameter	– 1.75mm
Diameter Tolerance (mm)	– 0.05
Density (g/cm3)	– 0.98
Shore Hardness	– 90 to 98 (Shore A)
Elongation at Break (%)	– 500
Flexibility	– ≥40%
Tensile Strength (MPa)	– 50
Impact Strength (KJ/m2,Izod)	– >3
Total Weight	– 1kg

CCTREE Red Flexible 1.75mm TPU Filament - Suggested Print Settings:
Print Temperature (°C)	– 190 to 220
Bed Temperature (°C)	– 0 to 50
Layer Thickness (microns)	– 100 to 400
Wall Thickness (microns)	– ≥30
Infill Speed (mm/s)	– 15 to 30
Travel Speed (mm/s)	– 40 to 70
Retraction Speed (mm/s)	– 20 to 30
Print Bed Adhesion	– BuildTak Recommended